[image: image9.png]V7s)
{21505



            

	0.60mm Height 0603 Package
Blue Chip LED

Technical Data Sheet


Part No.: YBH-S0603UBC-T6
Features:


Descriptions:

Applications:


Package Dimension:

[image: image1.wmf]Unit: mm

Tolerance: ¡À0.10mm

Polarity

Recommended Soldering Pad Dimensions

0.7 [0.028]

0.8 [0.032]

0.8 [0.032]

0.8 [0.032]

0.24 [0.009]

1.2 [0.047]

1 [0.039]

0.6 [0.024]

0.3 [0.012]

0.8 [0.032]

0.8 [0.032]

+

1. Soldering terminal may shift in x, y direction.

2. Polarity referring onto the cathode mark is reversed on the UR/HR/SR.

1.6 [0.063]

PCB

Resin

LED Die

Cathode Mark

Soldering Terminal

0.3 [0.012]

0.3 [0.012]


	Part No.
	Chip Material
	Lens Color
	Source Color

	YBH-S0603UBC-T6
	InGaN
	Water Clear
	Blue


Notes:
1. All dimensions are in millimeters (inches).

2. Tolerance is ± 0.10mm (.004″) unless otherwise specified.

3. Specifications are subject to change without notice.
Absolute Maximum Ratings at Ta=25℃
	Parameters
	Symbol
	Max.
	Unit

	Power Dissipation
	PD
	95
	mW

	Peak Forward Current

(1/10 Duty Cycle, 0.1ms Pulse Width)
	IFP
	100
	mA

	Forward Current
	IF
	25
	mA

	Reverse Voltage
	VR
	5
	V

	Electrostatic Discharge (HBM)
	ESD
	2000
	V

	Operating Temperature Range
	Topr
	-40℃ to +80℃

	Storage Temperature Range
	Tstg
	-40℃ to +85℃

	Soldering Temperature
	Tsld
	260℃ for 5 Seconds


Electrical Optical Characteristics at Ta=25℃
	Parameters
	Symbol
	Min.
	Typ.
	Max.
	Unit
	Test Condition

	Luminous Intensity *
	IV
	100
	130
	---
	mcd
	IF=20mA (Note 1)

	Viewing Angle *
	2θ1/2
	---
	130
	---
	Deg
	IF=20mA (Note 2)

	Peak Emission Wavelength
	λp
	---
	465
	---
	nm
	IF=20mA

	Dominant Wavelength
	λd
	---
	470
	---
	nm
	IF=20mA (Note 3)

	Spectral Line Half-Width
	△λ
	---
	25
	---
	nm
	IF=20mA

	Forward Voltage
	VF
	2.80
	3.40
	3.80
	V
	IF=20mA

	Reverse Current
	IR
	---
	---
	10
	µA
	VR=5V


Notes:

1. Luminous Intensity Measurement allowance is ± 10%.

2. θ1/2 is the off-axis angle at which the luminous intensity is half the axial luminous intensity.

3. The dominant wavelength (λd) is derived from the CIE chromaticity diagram and represents the single wavelength which defines the color of the device.
Typical Electrical / Optical Characteristics Curves

(25℃ Ambient Temperature Unless Otherwise Noted)

[image: image2.wmf]Spectrum Distribution

Relative Luminous Intensity (%)

Ta=25¡æ

0

400

100

Forward Current & Forward Voltage

Forward Current IF (mA)

Ta=25¡æ

2.8

0

10

20

30

40

50

3.0

3.2

3.4

3.6

3.8

4.0

Forward Voltage  VF (V)

300

500

600

700

800

Wavelength 

λ

p (nm)

75

50

25

Luminous Intensity &

Ambient Temperature

Relative Luminous Intensity (%)

1

1000

-60

Ambient Temperature Ta (¡æ)

100

10

-40

-20

0

20

40

60

80

100

Luminous Intensity & Forward Current

Relative Luminous Intensity (%)

1

1000

10

Forward Current IF (mA)

100

10

0

10

1

10

2

10

3

Forward Current Derating Curve

Forward Current IF (mA)

Ta=25¡æ

0

0

10

20

30

40

50

Ambient Temperature Ta (¡æ)

25

f=1KHz

Duty=1/10

Ta=25¡æ

20

40

60

80

100

Radiation Diagram

0.3

0

0.7

0.8

1.0

0.9

0.1

0

0.2

0.4

0.6

0.5

o

10

o

20

o

30

o

40

o

50

o

60

o

70

o

80

o

90

o


Reel Dimensions:
[image: image3.png]$13.0¢0.5

S'0F0'099
01508218

= 9.0%05
~— 12,0015





Carrier Tape Dimensions:
Loaded quantity 4000PCS per reel.
[image: image4.png]Progressive direction

4010
2.040.05 40 ®1.50.000 0.23+0.10

- Unit: mm
polarity Tolerance: +0.10 mm




CAUTIONS
1. Handling Precautions:

1.1. Handle the component along the side surfaces by using forceps or appropriate tools.

1.2. Do not directly touch or handle the silicone lens surface. It may damage the internal circuitry.

1.3. Do not stack together assembled PCBs containing exposed LEDs. Impact may scratch the silicone lens or damage the internal circuitry.

[image: image5.png]OlVI%1%,




Compare to epoxy encapsulant that is hard and brittle, silicone is softer and flexible. Although its characteristic significantly reduces thermal stress, it is more susceptible to damage by external mechanical force. As a result,special handling precautions need to be observed during assembly using silicone encapsulated LED products. Failure to comply might lead to damage and premature failure of the LED.
2. Storage

2.1. Do not open moisture proof bag before the products are ready to use.

2.2. Before opening the package, the LEDs should be kept at 30°C or less and 60%RH or less.

2.3. The LEDs should be used within a year.

2.4. After opening the package, the LEDs should be kept at 30°C or less and 60%RH or less.

2.5. The LEDs should be used within 24 hours after opening the package.

2.6. If the moisture adsorbent material has fabled away or the LEDs have exceeded the storage time, baking treatment should be performed using the following conditions. Baking treatment: 65±5°C for 24 hours.
3. Soldering Condition

3.1. Pb-free solder temperature profile

[image: image6.png]———®=— Temperature

300

Maximum Solder Profile __

°C Recommended Solder Profile
P Minimum Solder Profile
250 —| 255°¢
240°c
217°c
200
150 — Ramp Down
6 K/s(max)
120 S Max 100 S Max o
/ Ramp Up
3 K/s(max)
Sec
0 \ \ 1 I I
0 50 100 150 200 250 S 300




3.2. Reflow soldering should not be done more than two times.

3.3. When soldering, do not put stress on the LEDs during heating.

3.4. After soldering, do not warp the circuit board.

3.5. Recommended soldering conditions:

[image: image7.png]Reflow soldering

Soldering iron

Pre-heat

Pre-heat time

Peak temperature

Soldering time

150~200°C

120 sec. Max.

260°C Max.

10 sec. Max.(Max. two times)

Temperature

Soldering time

300°C Max.

3 sec. Max.

(one time only)





3.6. Because different board designs use different number and types of devices, solder pastes, reflow ovens, and circuit boards, no single temperature profile works for all possible combinations.

However, you can successfully mount your packages to the PCB by following the proper guidelines and PCB-specific characterization.

4. Drive Method

4.1. An LED is a current-operated device. In order to ensure intensity uniformity on multiple LEDs connected in parallel in an application, it is recommended that a current limiting resistor be incorporated in the drive circuit, in series with

each LED as shown in Circuit A below.

[image: image8.png]Circuit model A
LED

Circuit model B
LED

oO—

%ﬁ/ \ £

i L





a. Recommended circuit.

b. The brightness of each LED might appear different due to the differences in the I-V characteristics of those LEDs.

Terms and conditions for the usage of this document

1. The information included in this document reflects representative usage scenarios and is intended for technical reference only.

2. The part number, type, and specifications mentioned in this document are subject to future change and improvement without notice. Before production usage customer should refer to the latest datasheet for the updated specifications.

3. When using the products referenced in this document, please make sure the product is being operated within the environmental and electrical limits specified in the datasheet. If customer usage exceeds the specified limits,Baihui will not be responsible for any subsequent issues.

4. The information in this document applies to typical usage in consumer electronics applications. If customer's application has special reliability requirements or have life-threatening liabilities, such as automotive or medical usage, please consult with baihui representative for further assistance.

5. The contents and information of this document may not be reproduced or re-transmitted without permission by baihui
Package in 8mm tape on 7″ diameter reel.


Compatible with automatic placement equipment.


Compatible with infrared and vapor phase reflow solder process.


Mono-color type.


The product itself will remain within RoHS compliant Version.





The S0603-T6 SMD LED is much smaller than lead frame type components, thus enable smaller board size, higher packing density, reduced storage space and finally smaller equipment to be obtained.


Besides, lightweight makes them ideal for miniature applications, etc.





Automotive: Backlighting in dashboard and switch.


Telecommunication: Indicator and backlighting in telephone and fax.


Flat backlight for LCD, switch and symbol.


General use.








Spec No.: S0603-T6        Rev No.: V.3            Date: 2023-12-01          Page: 1 OF 9
E-mail: 499200972@qq.com                               

Guangzhoubaihuioptoelectonics technologyco.,ltd            http://www.ledbaihui.com

_1263052460.dwg

_1314689467.dwg

