[image: image4.png]V7s)
{21505



               


Part No.: YBH-R1012GB
Features:


Descriptions:


Applications:


Device Selection Guide:
	Part No.
	Chip Material
	Face Color
	Source Color

	YBH-R1012GB
	GaP
	Black Diffused
	Yellow Green


Package Dimension:
[image: image1.png]174 [0.069] 7.900311)
PIN 10 ‘ pne J903N
\+ | +, _ ——
= | 3 g
S T S =
= | = =
X+ : +\ Bt
PIN 1 — 125 [0.493] — PIN5 4] ,158]1L,5
AB CODE
- J H H H ©0.5[0.020) IIIII

t,54‘4: 10.16 [0.400




[image: image2.png]



Notes:

1. All dimensions are in millimeters (inches).

2. Tolerance is ± 0.25 mm (.010″) unless otherwise noted.

3. Specifications are subject to change without notice.

Absolute Maximum Ratings at Ta=25℃
	Parameters
	Symbol
	Max.
	Unit

	Power Dissipation
	PD
	84
	mW

	Peak Forward Current 

(1/10 Duty Cycle, 0.1ms Pulse Width)
	IFP
	100
	mA

	Forward Current
	IF
	30
	mA

	Dating Linear From 25℃
	
	0.25
	mA/℃

	Reverse Voltage
	VR
	5
	V

	Operating Temperature Range
	Topr
	-40℃ to +80℃

	Storage Temperature Range
	Tstg
	-40℃ to +85℃

	Soldering Temperature
	Tsld
	260℃ for 5 Seconds


Electrical Optical Characteristics at Ta=25℃
	Parameters
	Symbol
	Min.
	Typ.
	Max.
	Unit
	Test Condition

	Luminous Intensity
	IV
	2.5
	5.0
	---
	mcd
	IF=20mA (Note 1)

	Peak Emission Wavelength
	λp
	---
	568
	---
	nm
	IF=20mA

	Dominant Wavelength
	λd
	---
	572
	---
	nm
	IF=20mA (Note 2)

	Spectral Line Half-Width
	△λ
	---
	20
	---
	nm
	IF=20mA

	Forward Voltage
	VF
	---
	2.00
	2.20
	V
	IF=20mA

	Reverse Current
	IR
	---
	---
	10
	µA
	VR=5V


Notes:

1. Luminous intensity is measured with a light sensor and filter combination that 
approximates the CIE eye-response curve.
2. The dominant wavelength (λd) is derived from the CIE chromaticity diagram and 
represents the single wavelength which defines the color of the device.
Typical Electrical / Optical Characteristics Curves

(25℃ Ambient Temperature Unless Otherwise Noted)



[image: image3.wmf]Spectrum Distribution

Relative Luminous Intensity (%)

Ta=25¡æ

0

400

100

Forward Current & Forward Voltage

Forward Current IF (mA)

Ta=25¡æ

0

10

20

30

40

50

1.6

1.8

2.0

2.2

2.4

Forward Voltage  VF (V)

300

500

600

700

800

Wavelength 

λ

p (nm)

75

50

25

Luminous Intensity &

Ambient Temperature

Relative Luminous Intensity (%)

1

1000

-60

Ambient Temperature Ta (¡æ)

100

10

-40

-20

0

20

40

60

80

100

Luminous Intensity & Forward Current

Relative Luminous Intensity (%)

1

1000

10

Forward Current IF (mA)

100

10

0

10

1

10

2

10

3

Forward Current Derating Curve

Forward Current IF (mA)

0

0

10

20

30

40

50

Ambient Temperature Ta (¡æ)

25

f=1KHz

Duty=1/10

Ta=25¡æ

20

40

60

80

100

2.6

2.8

      

Please read the following notes before using the datasheets:

1. Over-current-proof

Customer must apply resistors for protection, otherwise slight voltage shift will cause big current change ( Burn out will happen ).

2. Storage

2.1 Do not open moisture proof bag before the products are ready to use.

2.2 Before opening the package, the LEDs should be kept at 30℃ or less and 90%RH or less.

2.3 The LEDs should be used within a year.

2.4 After opening the package, the LEDs should be kept at 30℃ or less and 70%RH or less.

3. Soldering Condition

3.1 Pb-free solder temperature profile.

3.2 Reflow soldering should not be done more than two times.

4. Soldering Iron

Each terminal is to go to the tip of soldering iron temperature less than 260℃ for 5 seconds 
within once in less than the soldering iron capacity 25W. Leave two seconds and more intervals, and do soldering of each terminal. Be careful because the damage of the product is often started
 at the time of the hand solder.

5. Repairing

Repair should not be done after the LEDs have been soldered. When repairing is unavoidable, a double-head soldering iron should be used. It should be confirmed beforehand whether the characteristics of the LEDs will or will not be damaged by repairing.

5 Segment Light Bars Displays


Technical Data Sheet





Industrial standard size.


Low power consumption.


Categorized for luminous intensity.


The product itself will remain within RoHS compliant Version.





The YBH-R1012 series is 5 Segment light bar display, designed for viewing distances up to 7 meters.





Audio equipment.


Instrument panels.


Digital read out display.





� EMBED Excel.Sheet.8  �錯誤! 內嵌物件無效。�








Spec No.: R1012                Rev No.: V.6           Date:2023-12-01           Page: 1 OF 6

E-mail: 499200972@qq.com                               

Guangzhoubaihuioptoelectonics technologyco.,ltd            http://www.ledbaihui.com

_1258272885.dwg

_1038911326.xls
I-V Curve

		2.007

		2.04

		2.063

		2.086

		2.107

		2.124

		2.141

		2.157

		2.171

		2.185

		2.2

		2.213

		2.225

		2.241

		2.251

		2.265

		2.278

		2.29

		2.3

		2.311

		2.324

		2.335

		2.344

		2.358

		2.369

		2.377

		2.39

		2.401

		2.411

		2.419

		2.433

		2.44

		2.452

		2.464

		2.472

		2.483

		2.497

		2.503

		2.515

		2.527

		2.535

		2.543

		2.555

		2.562

		2.572

		2.583

		2.591

		2.602

		2.612



1

Forward Voltage VF(V)

Forward Current IF(mA)

Forward Current 
vs Forward Voltage

2

3

4

5

6

7

8

9

10

11

12

13

14

15

16

17

18

19

20

21

22

23

24

25

26

27

28

29

30

31

32

33

34

35

36

37

38

39

40

41

42

43

44

45

46

47

48

49

50



I-LOP Curve

		1

		2

		3

		4

		5

		6

		7

		8

		9

		10

		11

		12

		13

		14

		15

		16

		17

		18

		19

		20

		21

		22

		23

		24

		25

		26

		27

		28

		29

		30

		31

		32

		33

		34

		35

		36

		37

		38

		39

		40

		41

		42

		43

		44

		45

		46

		47

		48

		49

		50



Forward Current IF(mA)

Relative Intensity (LOP@20mA=1)

Relative Luminous Intensity 
vs Forward Current

0.0392464678

0.0855572998

0.1357927786

0.1844583987

0.2346938776

0.2857142857

0.3359497645

0.3869701727

0.4379905808

0.489010989

0.5392464678

0.590266876

0.6412872841

0.6930926217

0.7448979592

0.795133438

0.8453689168

0.8971742543

0.9474097331

1

1.0502354788

1.1020408163

1.1514913658

1.2025117739

1.2543171115

1.3037676609

1.3555729984

1.4050235479

1.456043956

1.5070643642

1.5565149137

1.6083202512

1.6577708006

1.7080062794

1.7582417582

1.8076923077

1.8587127159

1.9081632653

1.9583987441

2.0078492936

2.057299843

2.1067503925

2.1562009419

2.2072213501

2.2551020408

2.3037676609

2.3532182104

2.4026687598

2.4529042386

2.5007849294



Wavelength Curve

		308.9

		312.125

		315.325

		318.55

		321.775

		325

		328.225

		331.45

		334.675

		337.925

		341.15

		344.4

		347.65

		350.9

		354.125

		357.375

		360.65

		363.9

		367.15

		370.425

		373.675

		376.95

		380.2

		383.475

		386.75

		390.025

		393.3

		396.575

		399.85

		403.125

		406.4

		409.675

		412.95

		416.25

		419.525

		422.825

		426.1

		429.4

		432.675

		435.975

		439.275

		442.575

		445.85

		449.15

		452.45

		455.75

		459.05

		462.35

		465.65

		468.95

		472.25

		475.55

		478.85

		482.15

		485.45

		488.75

		492.075

		495.375

		498.675

		501.975

		505.275

		508.6

		511.9

		515.2

		518.5

		521.8

		525.125

		528.425

		531.725

		535.025

		538.35

		541.65

		544.95

		548.25

		551.575

		554.875

		558.175

		561.475

		564.775

		568.075

		571.4

		574.7

		578

		581.3

		584.6

		587.9

		591.2

		594.5

		597.8

		601.1

		604.4

		607.7

		611

		614.3

		617.6

		620.9

		624.2

		627.475

		630.775

		634.075

		637.375

		640.65

		643.95

		647.25

		650.525

		653.825

		657.1

		660.4

		663.675

		666.975

		670.25

		673.55

		676.825

		680.1

		683.4

		686.675

		689.95

		693.225

		696.5

		699.8

		703.075

		706.35

		709.625

		712.9

		716.175

		719.45

		722.725

		725.975

		729.25

		732.525

		735.8

		739.075

		742.325

		745.6

		748.875

		752.125

		755.4

		758.65

		761.925

		765.175

		768.45

		771.7

		774.975

		778.225

		781.475

		784.75

		788

		791.25

		794.5

		797.775

		801.025

		804.275

		807.525

		810.775

		814.025

		817.3

		820.55

		823.8

		827.05

		830.3

		833.55

		836.8

		840.05

		843.3

		846.525

		849.775

		853.025

		856.275

		859.525

		862.775

		866.025

		869.275

		872.525

		875.75

		879

		882.25

		885.5

		888.75

		892

		895.25

		898.475

		901.725

		904.975

		908.225

		911.475

		914.725

		917.975

		921.225

		924.475

		927.725

		930.975

		934.225

		937.475

		940.725

		943.975

		947.225

		950.475

		953.725

		956.975

		960.25

		963.5

		966.75

		970.025

		973.275

		976.525

		979.8

		983.05

		986.325

		989.6

		992.85

		996.125

		999.4

		1002.675

		1005.95

		1009.225

		1012.5

		1015.775

		1019.05

		1022.325

		1025.6

		1028.9

		1032.175

		1035.475

		1038.75

		1042.05

		1045.35

		1048.65

		1051.95

		1055.25

		1058.55

		1061.85

		1065.15

		1068.475

		1071.775

		1075.1

		1078.425

		1081.75

		1085.075

		1088.4

		1091.725

		1095.075

		1098.4

		1101.75

		1105.075

		1108.425

		1111.775

		1115.15

		1118.5

		1121.85

		1125.225

		1128.6

		1131.975

		1135.35

		1138.725

		1142.1



Nanometers

Normalized
 Response

Spectral Radiance          Peak @636 nm

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0.0001342642

0.0002685285

0.0001342642

0.0002685285

0.0004027927

0.0009398496

0.0016111708

0.0018796992

0.0021482277

0.0025510204

0.0030880773

0.0036251343

0.0038936627

0.0044307197

0.0053705693

0.0053705693

0.0063104189

0.0063104189

0.0069817401

0.007518797

0.0081901182

0.009264232

0.0104726101

0.0124865736

0.0153061224

0.0187969925

0.0244360902

0.0320891515

0.0436358754

0.0592105263

0.0828410311

0.113453276

0.1554779807

0.208915145

0.2744360902

0.3591568206

0.4723415682

0.6338614393

0.8708378088

0.9989258861

0.9962406015

0.7504027927

0.4897959184

0.3202201933

0.2056928034

0.1337271751

0.0892857143

0.0610902256

0.0441729323

0.0323576799

0.0248388829

0.0197368421

0.0158431794

0.0136949517

0.0114124597

0.0099355532

0.0087271751

0.0079215897

0.0072502685

0.0064446831

0.005773362

0.0051020408

0.0042964554

0.004027927

0.0038936627

0.0037593985

0.0029538131

0.0024167562

0.0024167562

0.0018796992

0.001745435

0.0016111708

0.0009398496

0.0005370569

0.0005370569

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0

0



Data

		Electrical Characteristics

				LOP @ 20mA		VF1 @ 20mA		VF2 @ 10mA		VFD		VR @		IR

		1

		2

		3

		4

		5

		6

		7

		8

		9

		10

		11

		12

		13

		14

		15

		16

		17

		18

		19

		20

		AVG		0		0		0		0		0		0

		MIN		0.0		0		0		0		0		0

		MAX		0.0		0		0		0		0		0

				I-V Curve						I-LOP Curve								Spectral Radiance

				Forward Voltage		Forward Current				Forward Current		Relative Intensity		625 Readings				Nanometers		625 Readings		Normalized Response

				1.951		1				1		0.0392464678		0.05				308.9		0		0

				2.007		2				2		0.0855572998		0.109				312.125		0		0

				2.04		3				3		0.1357927786		0.173				315.325		0		0

				2.063		4				4		0.1844583987		0.235				318.55		0		0

				2.086		5				5		0.2346938776		0.299				321.775		0		0

				2.107		6				6		0.2857142857		0.364				325		0		0

				2.124		7				7		0.3359497645		0.428				328.225		0		0

				2.141		8				8		0.3869701727		0.493				331.45		0		0

				2.157		9				9		0.4379905808		0.558				334.675		0		0

				2.171		10				10		0.489010989		0.623				337.925		0		0

				2.185		11				11		0.5392464678		0.687				341.15		0		0

				2.2		12				12		0.590266876		0.752				344.4		0		0

				2.213		13				13		0.6412872841		0.817				347.65		0		0

				2.225		14				14		0.6930926217		0.883				350.9		0		0

				2.241		15				15		0.7448979592		0.949				354.125		0		0

				2.251		16				16		0.795133438		1.013				357.375		0		0

				2.265		17				17		0.8453689168		1.077				360.65		0		0

				2.278		18				18		0.8971742543		1.143				363.9		0		0

				2.29		19				19		0.9474097331		1.207				367.15		0		0

				2.3		20				20		1		1.274				370.425		0		0

				2.311		21				21		1.0502354788		1.338				373.675		0		0

				2.324		22				22		1.1020408163		1.404				376.95		0		0

				2.335		23				23		1.1514913658		1.467				380.2		0		0

				2.344		24				24		1.2025117739		1.532				383.475		0		0

				2.358		25				25		1.2543171115		1.598				386.75		0		0

				2.369		26				26		1.3037676609		1.661				390.025		0		0

				2.377		27				27		1.3555729984		1.727				393.3		0		0

				2.39		28				28		1.4050235479		1.79				396.575		0		0

				2.401		29				29		1.456043956		1.855				399.85		0		0

				2.411		30				30		1.5070643642		1.92				403.125		0		0

				2.419		31				31		1.5565149137		1.983				406.4		0		0

				2.433		32				32		1.6083202512		2.049				409.675		0		0

				2.44		33				33		1.6577708006		2.112				412.95		0		0

				2.452		34				34		1.7080062794		2.176				416.25		0		0

				2.464		35				35		1.7582417582		2.24				419.525		0		0

				2.472		36				36		1.8076923077		2.303				422.825		0		0

				2.483		37				37		1.8587127159		2.368				426.1		0		0

				2.497		38				38		1.9081632653		2.431				429.4		0		0

				2.503		39				39		1.9583987441		2.495				432.675		0		0

				2.515		40				40		2.0078492936		2.558				435.975		0		0

				2.527		41				41		2.057299843		2.621				439.275		0		0

				2.535		42				42		2.1067503925		2.684				442.575		0		0

				2.543		43				43		2.1562009419		2.747				445.85		0		0

				2.555		44				44		2.2072213501		2.812				449.15		0		0

				2.562		45				45		2.2551020408		2.873				452.45		0		0

				2.572		46				46		2.3037676609		2.935				455.75		0		0

				2.583		47				47		2.3532182104		2.998				459.05		0		0

				2.591		48				48		2.4026687598		3.061				462.35		0		0

				2.602		49				49		2.4529042386		3.125				465.65		0		0

				2.612		50				50		2.5007849294		3.186				468.95		0		0

																		472.25		0		0

																		475.55		0		0

																		478.85		0		0

																		482.15		0		0

																		485.45		0		0

																		488.75		0		0

																		492.075		0		0

																		495.375		0		0

																		498.675		0		0

																		501.975		0		0

																		505.275		4		0.0001342642

																		508.6		8		0.0002685285

																		511.9		12		0.0001342642

																		515.2		28		0.0002685285

																		518.5		48		0.0004027927

																		521.8		56		0.0009398496

																		525.125		64		0.0016111708

																		528.425		76		0.0018796992

																		531.725		92		0.0021482277

																		535.025		108		0.0025510204

																		538.35		116		0.0030880773

																		541.65		132		0.0036251343

																		544.95		160		0.0038936627

																		548.25		160		0.0044307197

																		551.575		188		0.0053705693

																		554.875		188		0.0053705693

																		558.175		208		0.0063104189

																		561.475		224		0.0063104189

																		564.775		244		0.0069817401

																		568.075		276		0.007518797

																		571.4		312		0.0081901182

																		574.7		372		0.009264232

																		578		456		0.0104726101

																		581.3		560		0.0124865736

																		584.6		728		0.0153061224

																		587.9		956		0.0187969925

																		591.2		1300		0.0244360902

																		594.5		1764		0.0320891515

																		597.8		2468		0.0436358754

																		601.1		3380		0.0592105263

																		604.4		4632		0.0828410311

																		607.7		6224		0.113453276

																		611		8176		0.1554779807

																		614.3		10700		0.208915145

																		617.6		14072		0.2744360902

																		620.9		18884		0.3591568206

																		624.2		25944		0.4723415682

																		627.475		29728		0.6338614393

																		630.775		29744		0.8708378088

																		634.075		29792		0.9989258861

																		637.375		29784		0.9962406015

																		640.65		29760		0.7504027927

																		643.95		29680		0.4897959184

																		647.25		22356		0.3202201933

																		650.525		14592		0.2056928034

																		653.825		9540		0.1337271751

																		657.1		6128		0.0892857143

																		660.4		3984		0.0610902256

																		663.675		2660		0.0441729323

																		666.975		1820		0.0323576799

																		670.25		1316		0.0248388829

																		673.55		964		0.0197368421

																		676.825		740		0.0158431794

																		680.1		588		0.0136949517

																		683.4		472		0.0114124597

																		686.675		408		0.0099355532

																		689.95		340		0.0087271751

																		693.225		296		0.0079215897

																		696.5		260		0.0072502685

																		699.8		236		0.0064446831

																		703.075		216		0.005773362

																		706.35		192		0.0051020408

																		709.625		172		0.0042964554

																		712.9		152		0.004027927

																		716.175		128		0.0038936627

																		719.45		120		0.0037593985

																		722.725		116		0.0029538131

																		725.975		112		0.0024167562

																		729.25		88		0.0024167562

																		732.525		72		0.0018796992

																		735.8		72		0.001745435

																		739.075		56		0.0016111708

																		742.325		52		0.0009398496

																		745.6		48		0.0005370569

																		748.875		28		0.0005370569

																		752.125		16		0

																		755.4		16		0

																		758.65		0		0

																		761.925		0		0

																		765.175		0		0

																		768.45		0		0

																		771.7		0		0

																		774.975		0		0

																		778.225		0		0

																		781.475		0		0

																		784.75		0		0

																		788		0		0

																		791.25		0		0

																		794.5		0		0

																		797.775		0		0

																		801.025		0		0

																		804.275		0		0

																		807.525		0		0

																		810.775		0		0

																		814.025		0		0

																		817.3		0		0

																		820.55		0		0

																		823.8		0		0

																		827.05		0		0

																		830.3		0		0

																		833.55		0		0

																		836.8		0		0

																		840.05		0		0

																		843.3		0		0

																		846.525		0		0

																		849.775		0		0

																		853.025		0		0

																		856.275		0		0

																		859.525		0		0

																		862.775		0		0

																		866.025		0

																		869.275		0

																		872.525		0		0

																		875.75		0		0

																		879		0		0

																		882.25		0		0

																		885.5		0		0

																		888.75		0		0

																		892		0		0

																		895.25		0		0

																		898.475		0		0

																		901.725		0		0

																		904.975		0		0

																		908.225		0		0

																		911.475		0		0

																		914.725		0		0

																		917.975		0		0

																		921.225		0		0

																		924.475		0		0

																		927.725		0		0

																		930.975		0		0

																		934.225		0		0

																		937.475		0		0

																		940.725		0		0

																		943.975		0		0

																		947.225		0		0

																		950.475		0		0

																		953.725		0		0

																		956.975		0		0

																		960.25		0		0

																		963.5		0		0

																		966.75		0		0

																		970.025		0		0

																		973.275		0		0

																		976.525		0		0

																		979.8		0		0

																		983.05		0		0

																		986.325		0		0

																		989.6		0		0

																		992.85		0		0

																		996.125		0		0

																		999.4		0		0

																		1002.675		0		0

																		1005.95		0		0

																		1009.225		0		0

																		1012.5		0		0

																		1015.775		0		0

																		1019.05		0		0

																		1022.325		0		0

																		1025.6		0		0

																		1028.9		0		0

																		1032.175		0		0

																		1035.475		0		0

																		1038.75		0		0

																		1042.05		0		0

																		1045.35		0		0

																		1048.65		0		0

																		1051.95		0		0

																		1055.25		0		0

																		1058.55		0		0

																		1061.85		0		0

																		1065.15		0		0

																		1068.475		0		0

																		1071.775		0		0

																		1075.1		0		0

																		1078.425		0		0

																		1081.75		0		0

																		1085.075		0		0

																		1088.4		0		0

																		1091.725		0		0

																		1095.075		0		0

																		1098.4		0		0

																		1101.75		0		0

																		1105.075		0		0

																		1108.425		0		0

																		1111.775		0		0

																		1115.15		0		0

																		1118.5		0		0

																		1121.85		0		0

																		1125.225		0		0

																		1128.6		0		0

																		1131.975		0		0

																		1135.35		0		0

																		1138.725		0		0

																		1142.1		0		0






